02300

Short Form Guide Specification

PERIMETER & BELOW-SLAB INSULATION

January 2002

2002 01 01

Dow Chemical Canada ULC

Short Form Guide Specification - Perimeter & Below-Slab Insulation

STYROFOAM™ Brand PERIMATE™/STYROFOAM™ Brand SM Extruded Polystyrene Foam

Insulation

SPEC NOTE: Following are suggested specification paragraphs to be used when specifying rigid board

insulation as perimeter insulation or below-slab insulation under Section 02300. Insert the required

paragraphs into the Section under the noted Articles, and make any required selections, such as board size,

thickness, etc. Where selection is indicated with an [OR] statement, select the appropriate paragraph and

delete the inappropriate statement. Delete all SPEC NOTE’s and [OR] statements prior to final printing.

DISCLAIMER: The manufacturer has reviewed the product information contained in this short form

specification and is responsible for its accuracy. The information is organized and presented to assist the

specification writer working on a construction project to select the appropriate products and to save time in

writing the project specification Section. The specification writer is responsible for product selection as

well as the use and application of this information, and should contact the manufacturer to ensure that all

options are available and that the associated specification information is valid and correct.

2.1 MATERIALS

.1 Perimeter Foundation Insulation: Extruded polystyrene foam insulation to CAN/ULC-S701,

Type 4, rigid, closed cell type, with integral high density skin, and vertical grooves designed to channel water down to the footing weep tile drains.

.1 Thermal Resistance: Long term aged RSI value of 0.87/25 mm, to ASTM C518.

.2 Board Size: [610 x 2440 mm, [53] [63] mm thick] [as indicated on Drawings].

.3 Compressive Strength: to ASTM D1621, minimum 210 kPa.

.4 Water Absorption: to ASTM D2842, 0.7% by volume maximum.

.5 Edges: Shiplapped.

.6 Drainage Capacity: >0.72 m3/hr/m, CCMC Class A, Type 2.

.7 Water Vapour Permeance: to ASTM E96, 50 ng/Pas m2 max.

.8 Manufacturer and Product Name: STYROFOAM™ Brand SM Extruded Polystyrene

Foam Insulation, Dow Chemical Canada ULC

[OR]

.1 Perimeter Foundation Insulation: Extruded polystyrene foam insulation to CAN/ULC-S701,

Type 4, rigid, closed cell type, with integral high density skin, c/w intergral 9 mm thick latex-

modified concrete facing.

.1 Thermal Resistance: Long term aged RSI value of 0.87/25 mm, to ASTM C518.

.2 Board Size: [610 x 1220 mm, 50 mm thick] [as indicated on Drawings].

.3 Compressive Strength: to ASTM D1621, minimum 210 kPa.

.4 Water Absorption: to ASTM D2842, 0.7% by volume maximum.

.5 Edges: Tongue and groove sides, square edge ends.

.6 Water Vapour Permeance: to ASTM E96, 50 ng/Pas m2.

.7 Manufacturer and Product Name: STYROFOAM™ Brand Extruded Polystyrene

Foam Insulation, Dow Chemical Canada ULC

.2 [Below-Grade] [Below-Slab] [Perimeter Foundation] Insulation: Extruded polystyrene foam

insulation to CAN/ULC-S701, Type 4, rigid, closed cell type, with integral high density skin.

.1 Thermal Resistance: Long term aged RSI value of 0.87/25 mm, to ASTM C518.

.2 Board Size: [600 x 1220 mm, 50 mm thick] [as indicated on Drawings].

.3 Compressive Strength: to ASTM D1621, minimum 210 kPa.

.4 Water Absorption: to ASTM D2842, 0.7% by volume maximum.

.5 Edges: [Square] [Shiplapped].

.6 Water Vapour Permeance: to ASTM E96, 50 ng/Pas m2.

.7 Manufacturer and Product Name: STYROFOAM™ Brand SM Extruded Polystyrene

Foam Insulation, Dow Chemical Canada ULC

2002 01 01

Dow Chemical Canada ULC

Short Form Guide Specification - Perimeter & Below-Slab Insulation

STYROFOAM™ Brand PERIMATE™/STYROFOAM™ Brand SM Extruded Polystyrene Foam

Insulation

.3 Adhesive: To CGSB 71-GP-24M, Type 1.

SPEC NOTE: Use the following two paragraphs when specifying concrete faced products.

.4 Metal Cap Flashing: 0.61 mm thick galvanized steel J-channel; 57 mm wide, 100 mm long leg

and 57 mm short leg; prefinished in colour selected by Consultant.

.5 Clips and Fasteners: corrosion-resistant type, sized to suit application; as supplied by insulation

manufacturer.

3 Execution

3.1 EXAMINATION

.1 Verify that the insulation boards and adjacent materials are compatible.

.2 Verify that substrate is flat, sound, clean, and free of oil, grease, [objectionable air surface

voids], [fins], [irregularities], [materials or substances that may impede adhesive bond].

3.2 PERIMETER INSULATION

.1 Apply adhesive in continuous 6 mm beads in a grid pattern to prevent potential air movement

behind the insulation boards. Apply adhesive fully around protrusions.

SPEC NOTE: Ensure extent of perimeter foundation insulation is indicated on drawings. Use the following

paragraph to specify exterior or interior applications.

.2 Install boards on [exterior] [interior] face of foundation [wall] [grade beam] perimeter,

[vertically] [horizontally]. Extend boards [minimum 600 mm [vertically from bottom of finish

floor slab] [below finish grade] [to top of footing].

.3 Place boards in a method to maximize contact with bedding. Stagger side and end joints. Butt

edges and ends tight to adjacent boards.

.4 Extend boards across control and expansion joints, unbonded to foundation 75 mm on one side

of joint.

.5 Cut and fit insulation tight to protrusions or interruptions to insulation plane.

SPEC NOTE: Use the following two paragraphs when installing concrete-faced insulation.

.6 Layout concrete-faced insulation boards to maximize board sizes. Do not use boards less than

150 mm wide.

.7 Install concrete-faced insulation board system [horizontally] [vertically], complete with

fastening clips and cap flashing in accordance with manufacturer’s installation guidelines.

3.3 BELOW-SLAB INSULATION

.1 Place insulation under slabs on grade after base for slab is complete. Lay boards on [level]

compacted fill.

2002 01 01

Dow Chemical Canada ULC

Short Form Guide Specification - Perimeter & Below-Slab Insulation

STYROFOAM™ Brand PERIMATE™/STYROFOAM™ Brand SM Extruded Polystyrene Foam

Insulation

.2 Extended boards [under entire area of slabs] [minimum 600 mm in from perimeter foundation

wall].

.3 Cut and fit insulation tight to protrusions or interruptions to insulation plane.

.4 Prevent insulation from being displaced or damaged while [placing vapour retarder and] placing

slab.

END OF SHORT FORM

®™Trademark of The Dow Chemical Company (“Dow”) or an affiliated company of Dow

Printed in U.S.A                                							             Form No. 178-00427-202QRP

McKAY200549