0721 5

Short Form Guide Specification

SPECIFYING INSULATION

DRAINAGE PANELS

This specification was prepared by

Charles E. Muire, FCSI, CCS

Joseph J . McGuire, FCSI, CCS

Indianapolis, Indiana								March 1997

March 1997

The Dow Chemical Company

Short Form Guide Specification- Insulation Drainage Panels

STYROFOAM™ Brand PERIMATE™ Extruded Polystyrene Foam Insulation

PART 1 - GENERAL

1.01	RELATED DOCUMENTS

A. Drawings and general provisions of Contract, including General and

Supplementary Conditions and Division-1 Specification Sections, apply to this

Section.

B. Backfilling is specified in Section 02220.

1.02	SUBMITTALS

A. Manufacturer's product literature including specified physical properties.

B. Installation instructions.

C. Certification that product complies with specification requirements and is

suitable for the use intended.

D. Manufacturer's thermal performance warranty.

1.03	QUALITY ASSURANCE

A. Insulating Drainage Panels shall not be produced with, or contain, any of the

United States EPA regulated CFC compounds listed in the Montreal Protocol

of the United Nations Environmental Program.

1.04	PRODUCT HANDLING

A. Protect insulating drainage panels from physical damage.

B. Comply with manufacturer's recommendations for handling, storage and

protection.

C. Handle boards carefully so corners are not broken off or boards otherwise

damaged.

March 1997

The Dow Chemical Company

Short Form Guide Specification- Interior Commercial Wall Insulation

STYROFOAM™ Brand PERIMATE™ Extruded Polystyrene Foam Insulation

1.05	WARRANTY

A. Provide written warranty that the actual thermal resistance of the extruded

polystyrene foam insulation will not vary by more than 10% from its published

thermal resistance.

B. Warranty period is 15 years after date insulation is purchased.

PART 2 - PRODUCTS

2.01	DRAINAGE BOARD

A. Material Properties:

1. Rigid closed-cell extruded polystyrene foam board with vertical channels

fabricated into one side, with shiplap edges.

2. Compressive Strength (ASTM D 1621-94): 30 psi.

***select appropriate subparagraph 3 below***

3. R-Value as per ASTM C 518-91: 5.0 (1.063" thick).

***or***

3. R-Value as per ASTM C 518-91: 10.0 (2.125" thick).

4. Water Absorption: Max. 0.3% by volume, ASTM C 272.

5. Surface Burning Characteristics:

a. Flame Spread: 5.

b. Smoke Developed: 165.

B. Acceptable manufacturer’s product: The Dow Chemical Company

STYROFOAM™ Brand PERIMATE™ Extruded Polystyrene Foam

Insulation.

2.02	ADHESIVE

A. Adhesive: mastic type recommended by insulating drainage panel

manufacturer as compatible with drainage panel and the waterproofing.

B. Acceptable manufacturer's products:

1. ChemRex, Inc. "Contech Brand PL300 Foam Board Adhesive".

2. ChemRex, Inc. "Contech Brand Premium Foam Board Adhesive".

3. Dacar Products, Inc. "Foamgrab PS".

March 1997

The Dow Chemical Company

Short Form Guide Specification- Interior Commercial Wall Insulation

STYROFOAM™ Brand PERIMATE™ Extruded Polystyrene Foam Insulation

PART 3 - EXECUTION

3.01	SURFACE PREPARATION

A. Surface shall be smooth, monolithic and free of coarse aggregate.

B. Clean off debris from footings.

C. Waterproofing shall be cured and free of solvent.

3.02	INSTALLATION

A. Before backfilling, completely cover damp-proofed or waterproofed wall with

insulation drainage panels.

B. Apply mastic adhesive in six 2" diameter equally-spaced daubs on the smooth

side of panels to adhere them to the cured waterproofing temporarily until

backfill is in place.

C. Install first panel vertically, with long edge flush with a comer.

1. Be sure shiplap on long edge of panel overlaps previous panel. Continue

until a comer is reached.

2. Cut and install comer panels, cutting off shiplap at corner.

D. When additional tiers are required, shiplap edges at both horizontal and

vertical joints.

E. Seal off top edge of panels below grade to prevent soil entry, using a J or Z

channel, sheathing tape, or soil fabric.

F. Protect exposed panels above grade from physical damage and ultraviolet

exposure with protection panel, flashing, or latex coating.

3.03 CLEAN-UP

A. Remove and dispose of excess panels, wrappings and other waste materials.

END OF SHORT FORM

Printed in U.S.A.                      ™® Trademark of The Dow Chemical Company (“Dow”) or an affiliated Company                     Form No. 179-04393-397

# Comments

Changed from 7.0

Changed from 1 ½”

Changed from 12

Changed from 2 ½